## Slide 1: Chapter 19: Thermal Properties
ISSUES TO ADDRESS...
• How do materials respond to the application of heat?
• How do we define and measure...
-- heat capacity?
-- thermal expansion?
-- thermal conductivity?
-- thermal shock resistance?
• How do the thermal properties of ceramics, metals, and polymers differ?

## Slide 2: Heat Capacity
• Quantitatively: The energy required to produce a unit rise in temperature for one mole of a material.
heat capacity
(J/mol-K)
energy input (J/mol)
temperature change (K)
• Two ways to measure heat capacity: Cp : Heat capacity at constant pressure.
Cv : Heat capacity at constant volume.
Cp usually > Cv
• Heat capacity has units of
The ability of a material to absorb heat

## Slide 3: Dependence of Heat Capacity on Temperature
• Heat capacity...
-- increases with temperature
-- for solids it reaches a limiting value of 3R
• From atomic perspective:
-- Energy is stored as atomic vibrations.
-- As temperature increases, the average energy of atomic vibrations increases.
Adapted from Fig. 19.2, Callister & Rethwisch 8e.
R = gas constant
3R
= 8.31 J/mol-K
Cv = constant
Debye temperature
(usually less than T
room
)
T (K)
q
D
0
0
Cv

## Slide 4: Atomic Vibrations
Atomic vibrations are in the form of lattice waves or phonons
Adapted from Fig. 19.1, Callister & Rethwisch 8e.

## Slide 5: Specific Heat: Comparison
increasing cp
• Why is cp significantly
larger for polymers?
Selected values from Table 19.1, Callister & Rethwisch 8e.
• Polymers
Polypropylene
Polyethylene
Polystyrene
Teflon
cp (J/kg-K)
at room T
• Ceramics
Magnesia (MgO)
Alumina (Al2O3)
Glass
• Metals
Aluminum
Steel
Tungsten
Gold
1925
1850
1170
1050
900
486
138
128
cp (specific heat): (J/kg-K)
Material
940
775
840
Cp (heat capacity): (J/mol-K)

## Slide 6: Thermal Expansion
Materials change size when temperature is changed
linear coefficient of
thermal expansion (1/K or 1/ºC)
Tinitial
Tfinal
 initial
 final
Tfinal > Tinitial

## Slide 7: Atomic Perspective: Thermal Expansion
Adapted from Fig. 19.3, Callister & Rethwisch 8e.
Asymmetric curve:
-- increase temperature, -- increase in interatomic separation -- thermal expansion
Symmetric curve:
-- increase temperature, -- no increase in interatomic separation -- no thermal expansion

## Slide 8: Coefficient of Thermal Expansion: Comparison
• Q: Why does a
generally decrease
with increasing
bond energy?
Polypropylene
145-180
Polyethylene
106-198
Polystyrene
90-150
Teflon
126-216
• Polymers
• Ceramics
Magnesia (MgO)
13.5
Alumina (Al2O3)
7.6
Soda-lime glass
9
Silica (cryst. SiO2)
0.4
• Metals
Aluminum
23.6
Steel
12
Tungsten
4.5
Gold
14.2
a (10-6/C) at room T
Material
Selected values from Table 19.1, Callister & Rethwisch 8e.
Polymers have larger  values because of weak secondary bonds
increasing 

## Slide 9: Thermal Expansion: Example
Ex: A copper wire 15 m long is cooled from 40 to -9ºC. How much change in length will it experience?
Answer: For Cu
rearranging Equation 19.3b

## Slide 10: Thermal Conductivity
The ability of a material to transport heat.
temperature
gradient
thermal conductivity (J/m-K-s)
heat flux
(J/m2-s)
• Atomic perspective: Atomic vibrations and free electrons in hotter regions transport energy to cooler regions.
T2
T2 > T1
T1
x1
x2
heat flux
Fourier’s Law

## Slide 11: Thermal Conductivity: Comparison
increasing k
• Polymers
Polypropylene
0.12
Polyethylene
0.46-0.50
Polystyrene
0.13
Teflon
0.25
vibration/rotation of chain molecules
• Ceramics
Magnesia (MgO)
38
Alumina (Al2O3)
39
Soda-lime glass
1.7
Silica (cryst. SiO2)
1.4
atomic vibrations
• Metals
Aluminum
247
Steel
52
Tungsten
178
Gold
315
atomic vibrations and motion of free electrons
k (W/m-K)
Energy Transfer Mechanism
Material
Selected values from Table 19.1, Callister & Rethwisch 8e.

## Slide 12: Thermal Stresses
• Occur due to:
-- restrained thermal expansion/contraction
-- temperature gradients that lead to differential dimensional changes
Thermal stress


## Slide 13: Example Problem
-- A brass rod is stress-free at room temperature (20ºC).
-- It is heated up, but prevented from lengthening.
-- At what temperature does the stress reach -172 MPa?
T0
 0
Solution:
Original conditions
Tf
Step 1: Assume unconstrained thermal expansion
 0
D
Step 2: Compress specimen back to original length
 0


D
Notes: 13

## Slide 14: Example Problem (cont.)
14
 0


The thermal stress can be directly calculated as
Noting that compress = -thermal and substituting gives
20 x 10-6/ºC
Answer: 106ºC
100 GPa
20ºC
Rearranging and solving for Tf gives
-172 MPa (since in compression)
Notes: 14

## Slide 15: Thermal Shock Resistance
• Occurs due to: nonuniform heating/cooling
• Ex: Assume top thin layer is rapidly cooled from T1 to T2
Tension develops at surface
Critical temperature difference
for fracture (set s = sf)
set equal
• Large TSR when is large
Temperature difference that
can be produced by cooling:
s
rapid quench
resists contraction
tries to contract during cooling
T2
T1
•

## Slide 16: Thermal Protection System
• Application:
Space Shuttle Orbiter
• Silica tiles (400-1260ºC):
-- large scale application
-- microstructure:
Fig. 19.2W, Callister 6e. (Fig. 19.2W adapted from L.J. Korb, C.A. Morant, R.M. Calland, and C.S. Thatcher, "The Shuttle Orbiter Thermal Protection System", Ceramic Bulletin, No. 11, Nov. 1981, p. 1189.)
Fig. 19.3W, Callister 5e. (Fig. 19.3W courtesy the National Aeronautics and Space Administration.)
Fig. 19.4W, Callister 5e. (Fig. 219.4W courtesy Lockheed Aerospace Ceramics
Systems, Sunnyvale, CA.)
reinf C-C
(1650ºC)
Re-entry T
Distribution
silica tiles
(400-1260ºC)
nylon felt, silicon rubber
coating (400ºC)
~90% porosity!
Si fibers
bonded to one
another during
heat treatment.
100 mm
Chapter-opening photograph, Chapter 23, Callister 5e (courtesy of the National Aeronautics and Space Administration.)

## Slide 17
THERMAL DIFFUSIVITY
It measures the ability of a material to conduct thermal energy relative to its ability to store thermal energy.It has the SI unit of m²/s. Thermal diffusivity is usually denoted by α
The formula is:
α = k/(c x rho )
where
k is thermal conductivity (W/(m·K))
rho is density (kg/m³)
c is specific heat capacity (J/(kg·K))

## Slide 18: Summary
The thermal properties of materials include:
• Heat capacity:
-- energy required to increase a mole of material by a unit T
-- energy is stored as atomic vibrations
• Coefficient of thermal expansion:
-- the size of a material changes with a change in temperature
-- polymers have the largest values
• Thermal conductivity:
-- the ability of a material to transport heat
-- metals have the largest values
• Thermal shock resistance:
-- the ability of a material to be rapidly cooled and not fracture
-- is proportional to

## Slide 19: ANNOUNCEMENTS
Core Problems:
Self-help Problems:
Reading: